| Grimwade Centre for Cultural Materials Conservation The University of Melbourne Victoria 3010 Tel: +61 3 8344 7989 Fax: +61 3 8344 0329 www.cultural-conservation.arts.unimelb.edu.au |  |
| --- | --- |

PROTOCOL FOR SAMPLING OF CULTURAL MATERIAL FOR SCIENTIFIC EXAMINATION

- CONTEXTUAL INFORMATION

- Research and consider art historical context.

- Compile information regarding artist's known materials and techniques.

- Compile additional documentary evidence where appropriate

- DEVELOP METHODOLOGY FOR SCIENTIFIC RESEARCH

- Primary sources: direct methods for the examination and characterization of materials and techniques. Methods may be invasive or non-invasive. Invasive techniques may be destructive, non-destructive, para-destructive.

- ‘Secondary’ sources: ‘indirect’ methods for the study of materials and techniques. References include treatises and receipt books; historical and archaeological reports; artists memoirs and interviews

- PRELIMINARY EXAMINATION AND DOCUMENTATION

- In situ technical examination of the artwork can be undertaken using non-invasive methods including diffuse light, raking light, ultra violet light, infrared reflectography, and the stereo microscope.

- A Condition Report should be completed for the work.

- JUSTIFICATION FOR SAMPLING

- Samples should be taken only be taken when preliminary non-invasive techniques have failed to adequately resolve questions pertinent to understanding of the work for the purposes of: authentication; identification of original and non-original materials; assessment of conservation issues and development of treatment strategies; understanding of the interaction between artistic expression and available materials etc.

- Prior to sampling the investigator should develop a general analytical pathway. The criteria under which this pathway is developed should consider the problem being investigated; selection of analytical methods most appropriate and relevant to resolution of the problem; efficiency, accuracy and cost effectiveness of the outlined approach

- APPROVAL OF SAMPLING

- Submit condition report and justification for sampling to owner, custodian of collection or supervisor.

- Submit ‘request for sampling form’ to the above and seek approval. Ensure the client signs the document before sampling is undertaken.

- Fill out the  sampling check list for conservators.

- SAMPLING METHODS

- If sampling is necessary the investigator should determine how to maximize information from the minimum amount of sample material

- Samples should be removed from an unobtrusive location and should be representative of the material/stratigraphy being investigated. Areas of non-original material should be avoided, unless specifically required

- Samples are normally taken with an opthamological scalpel from edges, losses, tears or cracks

- All sampling should be fully documented graphically and/or photographically and the appropriate proformas completed. At GCCMC fill out the sample registration form.

- All required materials an equipment should be prepared and assembled prior to sampling

- Contamination of the sample should be minimized: use clean blades etc. and have a clean glass phial (or other suitable container) ready to receive the sample clearly labeled with identification details (sample type, id number, artist, object, owner, date)

- Further preparation of the sample will be determined by the analytical technique selected

- Sample preparation: does this need to be undertaken in a specialist laboratory? will the sample be destroyed/altered during analysis? can tests be repeated? can samples be used for more than one method?